Microstrip Rectangular Patch Antenna Printed on LiTi Ferrite with Perpendicular DC Magnetic Biasing

Naveen Kumar Saxena1,* (IEEE Student Member), Nitendar Kumar2 and P.K.S. Pourush1

- Microwave Lab, Department of Physics, Agra College Agra 282002 (U.P) India.

Nav3091@rediffmail.com, ppourush@yahoo.co.in

- Solid State Physics Laboratory, Timarpur, Delhi 110007 India.

Nitendar@rediffmail.com

Abstract: Characterization of a tunable & switchable microstrip rectangular patch antenna printed on synthesized LiTi ferrite substrate with a normal magnetic bias field is presented. In this paper the concept of switching and tuning has been described by magnetostatic and spin waves phenomenon. The DC magnetic biasing generate these both type of waves which response a number of novel magnetic and electrical characteristics including switchable and polarized radiations from a microstrip antenna. In such a case of substituted polycrystalline ferrite antenna due to the DC biasing, most of the power will be converted into mechanical waves and little radiates into air. Under such condition the antenna become switch off, in the sense of effectively absence as radiator. The preparation of ferrite by the solid state reaction technique is also précised with the short description of electric and magnetic properties. [Journal of American Science 2010;6(3):46-51]. (ISSN: 1545-1003).

Index Terms: Substituted ferrite, microstrip patch antenna, magnetostatic waves, spin waves, X-band frequency range.

List of Symbols

fr	=		resonant frequency

h	=		height of substrate

λ      	=		wavelength

ai	=		inter-atomic space

s	=		side length of rectangular patch

βx , βy 	=	progressive phase excitation difference   along x and y direction respectively

dx , dx  =	element separation along x and y direction respectively

α    	=		attenuation constant

β	=		phase constant

βo	= 		propagation constant in vacuum

εr 	=		dielectric constant

µeff 	= 		effective permeability

µ, κ	=		permeability tensor components of µeff

T	= 		relaxation time

Ho	=		applied bias field

ΔH	= 		magnetic resonance width of ferrite

ω	= 		angular frequency of incident e-m-waves

ωo	= 		external magnetic field angular frequency

ωm	= 		internal magnetic field angular frequency

ωex	=	internal magnetic field angular frequency due to exchange forces

µ’	= 		real part of permeability

µ’’	= 		dissipative part of permeability

χ’	= 		real part of susceptibility

χ’’	= 		dissipative part of susceptibility

4πMS	=		saturation magnetization

ϒ	=		gyromagnetic ratio (2.8 MHz / Oe.)

- Introduction

In the present era of high frequency communication, ferrite is one of the important magnetic materials which are used as in both types single and polycrystalline. Some novel characteristics of polycrystalline ferrite over normal dielectric material make it very useful in microwave antenna applications. Different types of polycrystalline ferrites have their specific advantages as Li substituted ferrites has high dielectric constant, low sintering temperature etc. than other substituted ferrites. The reason for using ferrite materials in microstrip structures is that the applied magnetic field changes the permeability and thus the electrical properties of material, which in turn changes the antenna properties. The significance of this is that it is possible to change the antenna characteristics through the DC magnetic field applied externally (Pozar et al., 1993, 1992, 1988; Fukusako et al., 1998).

Beam steering, gain and bandwidth enhancement, RCS control, surface wave reduction, switchable and electronic tunability are some of the unique and inherent features of ferrite based microstrip antennas and arrays, which have been discussed by numbers of investigators for the C-band and S-band but not for the X-band (Dixit et al., 2000; Batchelor et al., 1997; Ufimtsev et al., 2000; Horsfield et al., 2000).

In the present paper, the concept of tunable antenna with the magnetostatic and spin wave has been developed by rectangular patch printed on LiTi ferrite substrate in the X band.

- Theory

The geometry of antenna is shown in fig. 1. The patch of length ‘L’ and width ‘W’ printed on LiTi ferrite substrate of thickness ‘h’. The dielectric constant and saturation magnetization () of substrate is 16 and 2200 Gauss respectively. There are many feeding techniques available but due to the brittleness of substrate stripline feeding is preferred.

Figure 1. Geometry of microstrip rectangular patch antenna.

Consider a plane wave propagating in the perpendicular direction of slab with a magnetic bias field applied longitudinally. As a result of elasticity of the spin (magnetic) system, oscillations (precession) of the magnetic moments with the frequency of exciting force can exist and they are in resonance for the frequency equal to μoγHi, where Hi is the internal field in the magnetic material. If these oscillations are excited in limited region of the ferrite sample, then due to elasticity of this system they will propagate with a defined velocity in the sample. This propagating disturbance represents magnetostatic and spin waves. These waves are generated when external magnetic field applied perpendicular to the magnetic vector of EM waves. MSW propagate perpendicularly on both sides to the EM wave’s propagation [Lax et at, 1962].

If we consider the infinite medium plane wave solution of the equations of motion including the spin wave “exchange” term and neglecting losses then the dispersion relation for ω as a function of k, for the biquadratic equation (4) is given by:

If we plot the dispersion relation (5) then we got-

a curve between frequency (ω) and propagation constant (k) for a particular value of external magnetic field (Ho). The value of propagation constant (k) becomes zero twice at which the frequency known as cutoff frequency which is due to the generation of three types of waves: quasi TEM, Magnetostatic and Spin waves. Spin wave excitation is the result of exchange forces between atoms. Magnetostatic waves are of two types (1) Surface MSW (2) Volume MSW (Lax et al, 1962; Kabos et al, 1994; Sodha et al, 1981).

- Surface MSW

Surface magnetostatic waves are the most common and well investigated class of magnetostatic waves. These waves propagate in ferromagnetic materials magnetized in the layer plane perpendicularly to the direction of the magnetic field. The classical dispersion equations first published by Damon and Eshbach in 1961, so that these wave also known as Damon-Eshbach waves. The dispersion relation of surface MSW with spin wave exchange term, given as follows:

Surface MSW band limits:

Surface MSW in metal coated ferrite:

- Volume MSW

These types of waves generally produce dominantly in the layered structure perpendicular to surface MSW propagation or magnetized layer. The dispersion relation of volume MSW with spin wave exchange term, given as follows:

Volume MSW band limits:

- Synthesis Of Substrate

LiTi ferrite synthesized from the basic components of lithium ferrites. The ingredients required for the preparation of these ferrites have been calculated on the basis of chemical formula. A small amount of Mn3+ ion has been also incorporated in the basic composition in order to suppress the formation of Fe2+ ions in the ferrites and to influence megnetostriction being a John Teller ion (Uitert et al., 1956; Kishan et al, 1985). In order to avoid Lithia at high temperature of sintering, Bi2O3 (0.25 wt %) has been added as sintering aid (Randhawa et al, 2007). Analytical grade chemicals have been used for the preparation of the material. The stoichiometric ratio of the chemicals has been thoroughly mixed in a polypropylene jar containing the zirconium balls and distilled water has been used as a mixing agent. The presintering of the mixed powder has been carried out at ~ 750oC in a box furnace and soaking time was kept 4 hours. The sieved material has been pressed in disk (antenna substrate) and toroidal shapes with the help of suitable dies and using hydraulic pressing technique at pressure of 10 ton/cm2. The substrates and toroidals have been finally sintered at 1050oC for four hours. The heating and cooling cycle of the samples has been carried out in the air atmosphere of furnace. The sintered samples so obtained have been subjected to cutting, grinding, polishing etc, in order to get specific size and shape.

The single-phase spinel nature of the samples has been confirmed by X-ray diffraction (XRD) patterns obtained by using Cu-Kα radiation. The microstructure studies of the sample have been carried out by scanning electron microscopy (SEM). Vibrating Sample Magnetometer (VSM) has been used to determine the magnetic properties of the samples. For dielectric measurements, rectangular pellets of size 25 mm  13 mm  7 mm have been used. The dielectric measurements have been performed from 8 to 12 GHz by a VNA E8263B Agilent Technology impedance analyzer. The value of the real part of dielectric constant () of the ferrite samples has been calculated using formula where ‘’ is the permittivity of free space = 8.85410-12 F/m, ‘C’ is the capacitance of specimen, ‘t’ is the thickness of specimen and ‘A’ is the area of sample in square meter. The density measurement has been done by a small experiment based on Archimedes' principle. Remanence and Coercive Force have been measured by B-H loop setup applied to coiled toroid sample at 50 Hz.

The Curie temperature for the LiTi ferrite samples has been determined by using a simple experimental setup based on gravity effect in the laboratory. The ferrite specimen has been made to attach itself to a bar magnet through a mild steel rod due to the magnetic attraction and combination was suspended inside the furnace. A chromel-alumel thermocouple has been attached with the sample holder to read the temperature of the specimen. As the temperature of the system was increased, at a particular temperature the specimen losses it spontaneous magnetization and become paramagnetic. This temperature is known as Curie temperature. At this temperature specimen fall downward due to gravity. The electrical and magnetic properties of LiTi ferrite substrate has been experimentally calculated in laboratory which is listed in table 1.

Table1. The electrical and magnetic properties of LiTi ferrite substrate

| LiTi Ferrite Characteristics | Values |
| --- | --- |
| Magnetic Saturation () | 2200 Gauss |
| Curie Temperature (Tc) | 500 K |
| Density (ρ) | 4.21 grams/cm3 |
| Remanence | 0.90 |
| Coercivity | 1.50 |
| Dielectric Constant (ε) | 17.5 |
| Resonance Line Width (∆H) | 370 Oersteds |
| Loss Tangent () | < 0.0005 |

- Simulation And Characterization

The dispersion curve for the material has been plotted and shown in fig. 2. It is clear from the curve that when ferrite substrate is magnetized the propagation constant (k) vary with frequency and the initial linear part of curve represents quasi TEM wave excitation which is of very small order (10-100) in comparison of scale (108). The rest part of curve represents MSW and Spin wave excitation. Spin wave excitation is the result of exchange forces between atoms.

According to Fig. 2 the absorbing power due to the MSW generation is in a particular limit. This particular limit depends upon the thickness of substrate, Resonance Line Width (ΔH) and external magnetic field orientation. Here obtained results are simulated and are in close agreement with results available in the literature.

The dimension of patch is calculated by following equations:

where

These equations are based on Transmission Line model. Symbol a, b, h, is the width, length and thickness of the patch respectively. To obtain good performance, there are many feeding methods, such as CPW in the ground feeding microstrip antenna, and CPW with stub patch feeding slot antenna (Bahl et al, 1980; Balanis et al, 1982).

Figure 2.	Dispersion curve (f vs. K) for plane wave propagation perpendicular to biasing field.

Thus the far zone expressions for rectangular patch microstrip antenna are obtained as follow:

where      Vo = voltage across the patch.

and

The polarization of antenna radiation can be decided by the propagation constant k as shown in table 2. The parameters related to patch characterization are calculated for biased and unbiased ferrite substrate, listed in table 3. By the help of these parameters and mathematical software (Mathworks MatLab 7.1), the radiation patterns are plotted in fig. 3 & 4 for E-plane and H-plane respectively for this geometry. These curves show a comparison between unbiased and biased substituted polycrystalline ferrite substrate patch antenna.

The total field pattern  is generally obtained from the relation [9-11]:

The value of  is computed for a case taking source frequency f=10 GHz, k= k+, , s = 0.2104 cm and loss tangent = 0.0005. For the array element separation  and progressive phase excitation is.

Table 2.	Antenna`s polarization function based on the propagation of magnetostatic and spin waves.

| Extraordinary Wave Propagation with Propagation Constant | Antenna Function |
| --- | --- |
| Negative | Off |
| Positive | Radiate with RHCP |
| Positive | Radiate with LHCP |

Table 3.	Comparison of Antenna`s parameters for Unbiased and biased case.

| Parameters | Unbiased | Biased |
| --- | --- | --- |
| Total Impedance (Zin) | 32.54 ohms | 83.52 ohms |
| Quality Factor (Q) | ~7 % | ~7 % |
| Bandwidth (BW) | ~3 dB | ~3 dB |
| Directivity Gain (D) | 3.5 | 7.6 |
| Radiation Power (Pr) | 7.7 mW | 3.0 mW |
| Efficiency | 49 % | 49 % |

Figure 3.	Comparison of E-plane pattern of rectangular patch microstrip antenna with RHCP for unbiased case and biased case.

Figure 4. Comparison of H-plane pattern of rectangular patch microstrip antenna with RHCP for unbiased case and biased case.

Conclusions

The integration of ferrite technology into microstrip printed circuit antenna has numerous advantages and potential applications. In this paper we have synthesized LiTi polycrystalline ferrite substrate using SSRT as a substrate for microstrip rectangular patch antenna at 10 GHz. of microwave frequency range. The parameters used for the study of biased ferrite substrate are saturation magnetization () = 2200 Gauss and bias field Ho= 1750 Oe. While, for unbiased ferrite substrate bias field become Ho= 0 Oe. The radiation patterns and antenna`s characteristics are calculated and reported in fig. 3, 4 and table 1, 2, 3 respectively.

It is evident from the dispersion effect on ferrite material that there should be a propagating and non-propagating region for an antenna. There is a frequency range bounded by limits, namely cutoff limit or resonance limit. In this where  is negative, the extraordinary wave is highly attenuating and   therefore the antenna is effectively off as radiator. Some salient features of this array geometry are summarized as follow:

- Comparison shows that on biasing, the radiation patterns becomes directive in nature. Directiveness can be observed by the comparison of E-plane pattern as shown in figure 3.

- It is evident from the dispersion curve that, for the given parameters, the cut-off limit is between 5 GHz. to 5.5 GHz. and tunable resonant region lies, except of the cutoff region. This property of antenna shows its switchable and tunable capability which can be varied as per requirement.

- When the antenna became biased with DC magnetic field the parameters show that the directivity gain is increased but the radiation power is decreased accordingly. Measurement also shows the increasing of total impedance in the case of external DC biasing.

- The size of patch is reduced considerable 35% comparable when designed on Quartz substrate. This reduction would certainly have a wide use in creating a miniaturization of an antenna system which has a potential application in space and cellular communication.

Acknowledgement

The authors are grateful to Dr. R Muralidharan, Director “Solid State Physics Laboratory, Timarpur, Delhi” for providing necessary facilities, encouragement and motivation to carry out this work.

Correspondence to:

Naveen Kumar Saxena (IEEE Student Member)

Microwave Lab, Department of Physics

Agra College Agra, 282002 (U.P) India.

Cellular Phone: 919411083091

Email: Nav3091@rediffmail.com

References

- Pozar DM, A magnetically switchable ferrite radome for printed antennas, IEEE Microwave and Guided Wave Letters 1993; MWL-3(3):67-69.

- Fukusako T, Seki Y and Mita N, Dispersion Characteristic of Microstrip Line using Ferrite Substrate Magnetized Longitudinally, Electronics Letters 1998; 34(16):1593-1594.

- Pozar DM, Sanchez V, Magnetic tuning of a microstrip antenna on a ferrite substrate, Electronic Letters, vol. 24, pp. 729-731, June 9, 1988.

- Pozar DM, RCS reduction for a microstrip antenna using a normally biased ferrite substrate. IEEE Microwave Guided Wave Letters 1992. 2:196-198.

- Dixit L, Pourush PKS, Radiation characteristics of switchable ferrite microstrip array antenna. IEE Proc. Microwave and Antennas Propagation 2000; 147(2):151-155.

- Batchelor JC, Langley RJ, Beam Scanning using Microstrip Line on Biased Ferrite. Electronic Letters 1997; 33(8):645-646.

- Ufimtsev PY, Ling RT, and Scholler JD, Transformation of surface waves in homogenous absorbing layers. IEEE Transaction on Antennas and Propagation 2000; 48:214-222.

- Horsfield B and Ball JAR, Surface wave propagation on grounded dielectric slab covered by a high-permittivity material. IEEE Microwave and Guided wave letters 2000; 10:171-173.

- Uitert Van LG, Mg-Fe3+ Spinels (Mg ferrites) and Mg-Fe3+ Spinels with Substitutions. Proc IRE 1956; 44:1294.

- Kishan Pran, Sagar DR, Chatterjee SN, Nagpaul LK, Kumar N, Laroia KK, Optimization of Bi2O3 Contents and its role in Sintering of Lithium Ferrite. Adv in Ceramics 1985; 16:207.

- Randhawa BS, Dosanjh HS, Kumar Nitendar, Synthesis of Lithium Ferrite by Precursor and Combustion Methods: A Comparative Study. Journal of Radio Analytical and Nuclear Chemistry 2007; 274(3):581-591.

- Lax B and Button K, Microwave Ferrite and Ferrimagnetics. McGraw-Hill, New York: 1962.

- Kabos P and Stalmachov VS, Magnetostatic Waves and their Applications. Chapman and Hall: 1994.

- Sodha MS and Srivastav NC, Microwave Propagation in Ferrimagnetics. Plenum Press, New York: 1981.

- Bahl IJ and Bhartia P, Microstrip Antennas. Artech House, Norwood, M.A: 1980.

- Balanis CA, Antenna Theory Analysis and Design. Harper & Row Publisher, New York (U.S.A.): 1982.

26/10/2009