Marsland Press

Journal of American Science 2009; 5(4):  71-78

Spectroscopic Characterization of Olivine [(Fe, Mg)2 SiO4] in Mahadevpur H4/5 ordinary chondrite

1,3 Bhaskar J. Saikia, 2G. Parthasarathy and 3N.C. Sarmah

1 G. B. Pant Institute of Himalayan Environment and Development, Almora - 263 643, India

2 National Geophysical Research Institute (CSIR), Hyderabad -500 007, India

3 Department of Physics, Dibrugarh University, Dibrugarh -786 004, India

(e-mail: vaskar_r@rediffmail.com)

Abstract

This study demonstrates for the first time, the spectroscopic characterization of Mahadevpur H4/5 chondrite that fell at Mahadevpur near Namsai town (Lat.27°40N, Long. 95°47E, Auranachal Pradesh, India) on 21 February 2007. The olivine group [(Mg, Fe)2SiO4] in Mahadevpur is characterized by the Fourier transform infrared (FT-IR), X-ray fluorescence (XRF) and Laser-Raman spectroscopic (RS) method. A comparison of results with Dergaon H5 chondrite is presented. Particular emphasis is given to the 10m (1000cm-1) and 20m (500 cm-1) region of infrared and Raman bands, which is originated from tetrahedral vibrations of silicates. [The Journal of American Science 2009; 5(4): 71-78]. (ISSN: 1545-1003).

Key words: Mahadevpur meteorite; olivine; spectroscopic characterization

- Introduction

Meteorites are fragments of rocks which originated from outer planetary bodies and fell on the surface of the earth. Meteorites can be divided into two major types, primitive and differentiated. Differentiated meteorites are igneous rocks that were crystallized from magmas generated at the interiors of their parent bodies. The primitive ones have not experienced the melting in their parent bodies, thus their bulk compositions, except for volatiles, are considered to represent those of the solar nebula where and when the meteorites formed. Since the majority of primitive meteorites have chondrules, they are commonly called chondrites. Chondritic meteorites are the oldest and most primitive rocks in the solar system. The primary divisions of chondrite classification are the carbonaceous, ordinary, and enstatite classes (Parthasarathy and Sarma, 2004). The chondrites are the most numerous meteorite group, accounting for 87% of all meteorites observed to fall. The largest group of chondritic meteorites is known as the ordinary chondrites, account for 80% of all known meteorites (Philip et al 2000).

http://www.americanscience.org americansciencej@gmail.com

71

Three subgroups of ordinary chondrites are identified, H group (high iron), L group (low iron), and LL group (low total iron, low metal). Chondrites contain small round masses of olivine or pyroxene. The silicates in meteorites predominantly consist of olivine and pyroxenes or non-crystalline silicates of intermediate compositions (Freund and Freund 2006).

On 21 February 2007, a meteorite fell Mahadevpur near Namsai town (Lat.27°40N, Long. 95°47E, Auranachal Pradesh, India) at 09:10 hrs Indian standard time (GMT+5:30hrs) (Weisberg et al 2008). The Mahadevpur meteorite is the forth documented meteorite from the north-eastern region of India. The last one was reported to fell on 2 March, 2001, at Dergaon and is classified as H5 chondrite (Grossman et al 2001). The other two are ‘Assam’ (1846) of type L5 and ‘Goalpara’ (1868) of type ureilite. The Mahadevpur meteorite has been documented as type H4/5 ordinary chondrite (Weisberg et al 2008). The present study represents the nature of olivine [(Mg,Fe)2SiO4] in Mahadevpur meteorite by comparing with Dergaon H5 chondrite.

Spectroscopic Characterization of Olivine [(Fe, Mg)2 SiO4] in Mahadevpur H4/5 ordinary chondrite                              Saikia et al

The olivine of Dergaon meteorite has reported by Gohainbarua (2003); Bhattacharyya (2004) (Gohainbarua et al 2003; Bhattacharyya et al 2004).  The comparative study of Mahadevpur is performed using X-ray fluorescence (XRF), Fourier transform infrared (FTIR) and Laser-Raman spectroscopy (RS). Particular interest is directed toward the 10μm (1000cm-1) and 20μm (500cm-1) region which exhibits the characteristics of olivine group.

2. Materials and Methods

A part of the meteorite samples (Figure 1) was crushed into fine powder by using agate mortar for analysis.  The X-ray fluorescence (XRF) data on the Dergaon and Mahadevpur meteorite were collected by using powdered homogenous sample in pellet form. For XRF studies a Philip Magix XRF spectrometer PRO model PW 2440 has been used in wavelength dispersive mode. Typical uncertainty involved is +/- 0.02 wt %. The thin sections of the sample have been characterized by electron microprobe analyzer. The experimental details were similar to that described elsewhere

(Bhandari et al. 2005; Dhingra et al. 2004). We tried to minimize the grinding time to avoid the deformation of the crystal structure, the ion exchange and the water absorption from atmosphere. The powdered sample was homogenized in spectrophotometric grade KBr (1:20) in an agate mortar and was pressed 3mm pellets with a hand press. The infrared spectra was acquired using Perkin-Elmer system 2000 FTIR spectrophotometer with helium-neon laser as the source reference, at a resolution of 4 cm-1. The spectra were taken in transmission mode in the region 400-4000 cm-1. The room temperature was 27°C during the experiment.

Raman spectrum is recorded using a Perkin-Elmer System 2000 FT-Raman spectrometer. For Raman microscopy a 50x objective was used and the spectra were excited by the 633 nm line of a He-Ne laser operating at 8 mW at the sample. The excitation laser for the FT-Raman spectra was a Nd:YAG laser of 1064nm wavelength, which could be operated at powers up to 500mW, but 150-250 mW for the high-pressure phases to avoid overheating the samples. Depending on fluorescence of the sample and acquisition times were between 120 and 180s. Slit widths were near 2 cm -1.

- (b)

Figure 1: The photograph of the studied meteorite samples. (a) Dergaon H5 chondrite (b) Mahadevpur H4/5 chondrite.

3. Results

The elemental composition of Dergaon and Mahadevpur chondrite by X-ray fluorescence (XRF) using the Dhajala (H3) meteorite as a standard. The classification, petrological and chemical characteristics of the Dergaon has been reported by Shukla et al 2005 (Shukla et al 2005). The elemental composition of Mahadevpur is compared with standard literature of Mason (1962) and Dergaon H5 chondrite which is listed in Table1. The elements of Mahadevpur are well agreement with the Mason (1962) and Dergaon results. The elemental ratio is compared with results of Aderson (2007) and Dergaon (Table 2). Olivine is the most abundant mineral in chondrites, followed by hypersthene, feldspar, nickel-iron, troilite and diopside

http://www.americanscience.org americansciencej@gmail.com

72

Marsland Press

Journal of American Science 2009; 5(3):  71-78

with minor apatite, chromite and ilmenite. The composition of the olivine varies widely, from 0 to 30 wt% Fe2SiO4 (Fa) (Mason 1962; Anderson 2007). Generally chondrites are distinguished by Mg/Si ratios. The Mg/Si ratio of Mahadevpur is indicative to the

type-H (Table 2). The olivine compositions of the two meteorites are presented in Table 3. The mineralogical phases of olivine in Mahadevpur meteorite is: olivine (Fo80.8 Fa19.3), orthopyroxene (En81 Fs17 Wo1), and clinopyroxene (En58 Fs8 Wo35).

Table1: Major elements observed in Dergaon and Mahadevpur meteorite. The elements of the studied meteorites are compared with the data obtain by Mason (1962) for H chondrite.

| Sample | Element (wt%) |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Si | Mg | Ca | Al | Fe | Ni | Co | Cr | K | P | Na | Ti |
| H chondrite * | 17.08 | 14.10 | 1.26 | 1.22 | 27.81 | 1.64 | 0.09 | 0.29 | 0.08 | 0.15 | 0.64 | 0.06 |
| Dergaon | 17.30 | 14.26 | 1.19 | 1.20 | 27.73 | 1.75 | -- | 0.03 | 0.067 | 0.15 | 0.670 | 0.04 |
| Mahadevpur | 16.90 | 14.10 | 1.19 | 1.32 | 28.40 | 1.67 | 0.07 | 0.20 | 0.075 | 0.12 | 0.052 | 0.04 |

Table 2: Comparison of elemental ratio of Dergaon, and Mahadevpur with the data of Aderson (2007) for  a standard H chondrite.

| Sample | Elemental ratio (wt%) |  |  |  |
| --- | --- | --- | --- | --- |
|  | Al/Si | Mg/Si | Ca/Al | Cr/Mg |
| H chondrite (standard) * | 0.063 | 0.800 | 1.110 | 0.025 |
| Dergaon | 0.069 | 0.824 | 0.992 | 0.002 |
| Mahadevpur | 0.078 | 0.834 | 0.084 | 0.014 |

Table 3: Olivine composition of Dergaon and Mahadevpur meteorite.

| Oxides ( wt%) | Dergaon-1 | Dergaon-2 | Dergaon-3 | Mahadevpur-1 | Mahadevpur-2 | Mahadevpur-3 |
| --- | --- | --- | --- | --- | --- | --- |
| SiO2 | 39.030 | 38.900 | 39.297 | 37.500 | 36.300 | 36.230 |
| Cr2O3 | 0.047 | 0.047 | -- | 0.026 | 0.026 | 0.026 |
| FeO | 18.400 | 18.734 | 18.999 | 18.650 | 18.650 | 18.470 |
| MnO | 0.455 | 0.475 | 0.465 | 0.100 | -- | -- |
| MgO | 41.372 | 41.512 | 41.774 | 43.600 | 44.320 | 44.800 |
| NiO | -- | -- | 0.063 | 0.070 | 0.010 | -- |
| CaO | 0.294 | -- | 0.261 | -- | 0.150 | -- |
| Total | 99.568 | 99.668 | 100.859 | 99.946 | 99.456 | 99.526 |

The silicates in primitive meteorites carry important information about cosmic silicates and their modification in the solar system. Strong emission and absorption features found around 9.7m and 18 μm, produced by Si-O stretching and O-Si-O bending modes, respectively. The 18 μm band is additionally broadened due to the coupling of the bending mode to the metal-oxygen stretching vibration located in this spectral region.

http://www.americanscience.org americansciencej@gmail.com

The position of the Si-O stretching vibration depends on the level of SiO4 polymerization. Generally, the spectrum can be divided into three main spectral regions. The bands between 1100 and 800 cm−1 correspond to different asymmetric and symmetric stretching vibrations of the SiO4 tetrahedra. The various features between 700 and 470 cm−1 are caused by bending vibrations of the SiO4 tetrahedra.

73

74

73

73

Spectroscopic Characterization of Olivine [(Fe, Mg)2 SiO4] in Mahadevpur H4/5 ordinary chondrite                              Saikia et al

The far-infrared bands in the low-frequency region beyond 470 cm−1 can be attributed to translational motions of the metal cations within the oxygen cage and complex translations involving metal and Si atoms.

The comparison of olivine group (Gadsden 1975) with Dergaon and Mahadevpur meteorite is presented in the Table 2.  Generally free SiO4 ion has exhibit four fundamental vibrational modes: a symmetric stretch (v1); a symmetric bend (v2); an asymmetric stretch (v3) and an asymmetric bend (v4). The infrared spectra of Dergaon and Mahadevpur meteorite in the 10μm and 20μm region are shown in the Figure 2. The strong bands in the 10μm (800-1150cm-1) region is identified as Si-O stretching and the bands present in the 20μm (400-700cm-1) region is assigned as Si-O-Si bending vibrations. The decreasing intensities in the Si-O stretching and Si-O-Si bending region are observed at  1053, 1012, 935, 920, and 504 cm-1  and 1059, 1002, 944, 927, and 506 cm-1 for Dergaon and Mahadevpur meteorite respectively, which are  identical to the bands of fayalite (Fe2SiO4), the bands found at 407, 467, 506, 601, 839, 988 and 1002 cm-1  in Mahadevpur infrared spectra and 467, 504, and 1012 cm-1    in Dergaon infrared spectra are identical to the bands of forsterite (Mg2SiO4) and the infrared bands  410, 506, 537, 694,  725, 927, 973, 1059, 1121 cm-1  and 504, 537, 724, 920, 976, 1012, 1053, 1122 cm-1 observed at Mahadevpur and Dergaon infrared spectra respectively are identical to the bands of enstatite (Mg2SiO3) (Gadsden1975). The band found at 506.0 cm-1 can be interpreted as Si-O and Mg-O vibrational modes in enstatite (MgSiO3) with slight shifts in the matrix (Nakamoto 1978). The petrologic type-5 chondrites have two strong peaks at 973 cm–1 and 535 cm–1 which may be related to Fe-O and Mg-O stretching modes (Nyquist et al 1971). The existence of these two peaks is found in Mahadevpur infrared spectra in weak and medium intensities.

The Figure 2 displaying clear Raman lines attribute to olivine in the meteorites. Generally olivine has 81 numbers of optic modes, out of which 36 numbers are Raman-active (Chopelas 1991; Hofmeister 1987). The Raman spectra (Figure 2) are divided into three regions as: below 400 cm-1; 400– 800 cm-1 (20μm); and 800–1100 cm-1(10μm). It may be noted that 20μm Raman bands are relatively weak as compare to their infrared counterparts. The peaks between 800 and 1100 cm-1 are attributed to SiO4 internal stretching vibrational modes; the dominant feature in this region is a doublet with

http://www.americanscience.org americansciencej@gmail.com

74

peaks near 818 and 852 cm-1. The relative heights of these peaks are a function of crystal orientation (Ishii 1978). These peaks result from coupled symmetric (v1) and asymmetric (v3) vibrations of SiO4 tetrahedra (Piriou and McMillan 1983; Chopelas 1991; Hofmeister 1987; Paques-Ledent and Tarte 1973; Lam et al 1990). The peaks in the 400–800 cm-1 region are the SiO4 internal bending vibrational mode.

Figure 2: Infrared and Raman spectra of Dergaon and

Mahadevpur meteorite in 10µm (800-1150cm-1), 20µm

(400-700cm-1) and below 400 cm-1 region.

Marsland Press

Journal of American Science 2009; 5(3):  71-78

The peaks below 400 cm-1 are mostly contributed by lattice modes: rotations and translations of SiO4 units and translations of octahedral cations in the crystal lattice (Chopelas 1991). These are weaker peaks, not often resolved in multi-phase spectra so only the doublet in the 800 –1100 cm-1 region is used in the calibration. In the studied meteorite samples, weak olivine bands are observed at 916-921 and 965-966 cm-1. The other bands at 249, 312-324, 336-344, 366 and 602-610, cm-1 correspond to pyroxene.

In the infrared spectrum the Si-O asymmetric stretching vibration (TO2-T2O5) is observed in between the peaks 1112-1003 cm-1. In between the peak position 920-988 cm-1 and 885-884 cm-1 the meteorites exhibits Si-O asymmetric vibration (TO3) and (T2O7--TO4) respectively. In the bending vibration region, the

symmetrical bending vibration of O-Si(Al)-O is observed at the peak position 685-682 cm-1. Another peak is observed at 463-462 cm-1 which is due to Si-O-Si bending vibration. In the Raman spectrum strong Si-O symmetric stretching bands appear at 813-823 and at 852-852 cm-1, and a medium-intensity antisymmetric Si-O stretching band appears at 965-966 cm-1 due to fosterite (Fo). The peaks of the 813-852 cm-1 doublet is assigned to a mixed contribution of the symmetric (ν1) and asymmetric (ν3) stretching modes of Si-Onb bonds (Non-Bridge Oxygen, NBO) in SiO4 tetrahedra (Lam et al 1990). This peak position may shift upwards as the values of Fo increase (Chopelas1991). The value Fo= Mg/(Mg+Fe) of an olivine can be determined from the XRF results. The peak 811-823 cm-1 has a higher contribution of ν3 (asymmetric mode) than the 852 cm-1 peak. This mode is more easily affected by variations

Table 4: Comparative spectral position of IR and RS in 10µm and 20µm region indicates fayalite, forsterite and enstatite in Dergaon and Mahadevpur meteorite. The infrared data of Gadsden (1975) and Raman data of Griffith (1975), White (1975) is taken as standard for fayalite, forsterite and enstatite spectral position analysis.

Fayalite      	     Forsterite       	      Enstatite	        Dergaon                  Mahadevpur

(Fe2SiO4)     	     (Mg2SiO4) 	      (Mg2SiO3)

IR	Raman	     IR	     Raman     IR	     Raman       IR	      Raman        IR	         Raman

( cm-1)     ( cm-1)	     ( cm-1)     ( cm-1)	      ( cm-1)       ( cm-1)      ( cm-1)    ( cm-1)         ( cm-1)    ( cm-1)

--	--	     --	       -- 	     1128-04     --	        1112       -- 	          1110        --

1060	--	     --	       --	     1070-56     --	        1052       --	          1057        --

--	--	     1000-990   --	     1020-10     --	        1012       --	          1003        --

--	--	     --	       964	     --	       --  	        --	       --	           --	          --

965-55	--	     965-58       --	     980-70       --	        982	       963	          988          966

950-47	--	     --	       --	     942-28       938	        932	       --	          945          --

920-15	--	     --	       919	     908-02       --	        --	       919	          920          916

880-73	--	     890	       --	     877-52       --	        885	       --	          884          880

--	838	     840	       855	     --	       863	        --	       852	          839          852

828	815	     --	       824	     --	       758	        --	       818	          --	          813

--	--	     --	       --	     728-19       715	        721	       --	          724          --

--	--	     --	       --	     695-93       681	        682	       --	          685          --

--	608	     620-02       608	     --	       650	        634	       610	          636          602

--	--	     --	       589	     --	       --	        593	       582	          596          --

566-58	550	     545	       --	     --	       545	        --	       --	          --	          --

--	--	     524	       544	     535	       523	        537	       547	          537          549

510-02	--	     512-01       --	     505	       --	        504	       --	          504          --

482-80	--	     473-63       --	     460	       --	        462	       --	          463          467

--	--	     430-28       434	     --	       --	        431	       430	          429          432

--	--	     409-05       --	     410	       --	        409	       --	          405          427

--	--	     --	       --	     397	       --	        366	       --	          360          --

380	--	     374	       --	     375	       --	        336	       --	          344          --

--	--	     317	       --	     340	       --	        312	       --	          324          --

--	--	     --	       234	     249	       --	        247         --	          --	          --

--	--	     --	       --	     --	       --	        --	       181	          --	          --

http://www.americanscience.org americansciencej@gmail.com

75

Spectroscopic Characterization of Olivine [(Fe, Mg)2 SiO4] in Mahadevpur H4/5 ordinary chondrite                              Saikia et al

in the Si-Onb force constant, and is also affected by the breakdown of SiO4 during polymerization (Lam et al 1990). The medium intensity peak in the region 547-610 cm-1 occurs due to the bridging oxygen (BO). The medium intensity peak at 916-921 cm-1 is indicative of the polymerization. The relative peak height is a function of crystal orientation (Ishii 1978). Therefore, the systematic variations of the high-frequency Si-O bands are attributed to decreased distortion of SiO4 tetrahedra.

4. Discussions

This is the first spectroscopic characterization of Mahadevpur H4/5 chondrite. The olivine group is identified from the compositional analysis, and is identical to the infrared and Raman results. The olivine composition of both meteorites is almost similar to each other. The strong IR and Raman absorption bands are due to olivine. It may be noted that in 20μm region Raman bands are relatively weak as compare to their infrared counterparts which is due to pyroxene.

Acknowledgements

We thank Directors, National Geophysical Research Institute, Hyderabad, and Indian Institute of Chemical Technology, Hyderabad for providing analytical facilities for characterization of the meteorites. One of us (GP) is grateful to ISRO, Department of space, Government of India, for partial financial support under PLANEX program. The authors are thankful to Prof. S. V. S. Murty, Physical Research Laboratory, Ahmedabad for his valuable discussions. Dr. P. K. Baruah, Gauhati University, Guwahati is thanked for his assistance with the infrared analysis. Special thanks to Dr. N. K. Gogoi, NGRI-Project Office, Tezpur for his cooperation in sample collection and Mr. P.K. Bhuyan, Superintendent of Police, Tinsukia, Assam for supplying the Mahadevpur meteorite specimen for study.

Correspondence to:

Bhaskar J. Saikia , e-mail: vaskar_r@rediffmail.com

References

1.  Anderson, D. L., New Theory of Earth, Cambridge

University Press, United Kingdom, 2007; 23-24

2.  Bhandari, N., Murthy, S.V.S., Shukla, P.N., Mahajan,

R.R., Shukla, A.D., Suthar, K.M., Parthasarathy, G., and

Paliwal, B.S., Bhawad, LL6 chondrite : Chemistry,

Petrology, noble gases, nuclear tracks, and cosmogenic

radionuclides, Meteoritics and Planetray Sciences 2005,

40: 1015-21

http://www.americanscience.org americansciencej@gmail.com

76

3.  Bhattacharyya, S., Gohainbarua,A., Knowar,

R.,Changmai, R., Baruah, G. D., Nature of the emission

band of Dergaon meteorite in the region 5700-6700Å,

Pramana, 2004; 62: 1299-01

4.  Chopelas, A., Single crystal Raman spectra of forsterite,

fayalite, and monticellite. American Mineralogist

1991; 76: 1101–09

5.  Dhingra, D., Bhandrai, N., Shukla, P.N., Murty, S.V.S.,

Mahajan, R.R., Ballabh, G.M., Lashkari, G., Shukla, A.D.,

Parthasarathy, G., Spectacular fall of the Kendrapara H5

chondrite, Meteoritics and Planetary Sciences 2004; 39:

A121-32

- Freund, M. M., Freund, F. T., Solid solution model for I

interstellar dust gains and their organics. The  Astrophy. J.

2006; 639: 210-26

- Gadsden, J. A., Infrared spectra of Mineral and related

Inorganic Compounds. USA: Butterworths. 1975;

165-90

8.   Gohainbarua, A. Barua, B. P., Bhattachyya, S., Baruah,

G. D., Spectroscopic investigation of Dergaon

meteorite with reference to 10m and 20m bands.,

Pramana 2003;  60: 47-52

9.   Griffith, W.P., Raman spectroscopy of Terrestrial

minerals in Infrared and Raman Spectroscopy of Lunar

and Terrestrial Minerals, Clarence Karr, Jr.(Ed),

Acadimic Press, New York, 1975: 299-23

10. Grossman, J.N., Zipfel, J. ,The Meteoritical Bulletin,

No.85, 2001, Sept. Meteritics & Planetary Science 2001;

36: A293-22

11. Hofmeister, A.M., Single-crystal absorption and

reflection infrared spectroscopy of forsterite and fayalite.

Physics and Chemistry of Minerals, 1987; 14:  499–13

12. Iishi, K., Lattice dynamics of forsterite. American

Mineralogist 1978; 63: 1198-08

13. Lam, P.K., Yu, R., Lee, M W., and Sharma, S K.,

Relationship between crystal structure and vibrational

mode in Mg2SiO4. American Mineralogist 1990; 75: 109-

l9

14. Mason, B., Meteorites, Jhon Wiley and Sons, New York,

1962: 65

15. Nakamoto K., Infrared and Raman Spectra of Inorganic

and Coordination Compounds, New York, John Wiley &

Sons, 1978: 105-39

16. Nyquist, R. A. & Kagel, R. O., Infrared Spectra of

Inorganic Compounds, 3800-45cm-1 , Academic Press:

New York, 1971: 16

17. Paques-Ledent, M, .Th., and Tarte, P., Vibrational studies

of olivine- type compounds. I. The i.r and Raman

spectra of the isotopic species of Mg2SiO4.

Spectrochimica Acta 1973; 29 A: 1007-16

input.doc

18. Parthasarathy, G and Sarma, S. R., High-temperature

electrical and thermal properties of Burdett, Dalhart,

Faucet and Wellman ordinary chondrites, Curr. Sci. 2004;

86(10): 1366-68

19. Philip, A.B., Alex W.R. B., Tim Jull, A. J., Ancient

Meteorite Finds and the Earth’s Surface Environment,

Quaternary Research 2000;  53: 131–42

20. Piriou, B., and McMillan, P., The high frequency

vibrational spectra of vitreous and crystalline

orthosilicates. American Mineralogist, 1983; 68: 426-43

21.  Shukla, P.N., Shukla, A.D., Rai,V.K., Murthy, S.V.S.,

Bhandari, N., Goswami, J.N.,Mazumder,A.C., Phukon,

K., Duorah, K.,Greenwood,R.E.,and Franchi,I.A., The

Dergaon (H5) chondrite: Fall, classification, petrological

and chemical characteristics, cosmogenic effects, and

noble gas records, Meteoritics & Planetary Science,

2005; 40: 627–37

6/20/2009

http://www.americanscience.org americansciencej@gmail.com

77

22. White, W.B., Structural interpretation of Lunar and

Terrestrial minerals by Raman spectroscopy, in Infrared

and Raman Spectroscopy of Lunar and Terrestrial

Minerals, Clarence Karr, Jr.(Ed),Academic Press, New

York, 1975; 325-58

23. Weisberg, M. K., Smith, C., Benedix. G., Foloco.

L., Righter, K., Zipfel, J., Yamaguchi, A., and

Chennaouiaoudjehane, H., The Meteoritical

Bulletin, No. 94. September 2008, Meteoritics &

Planetary Science 2008; 43(9): 1551–1588

Normal paper structure for the Journal of American Science

Each manuscript is suggested to include the following components but authors can do their own ways:

(1) The complete article title.

(2) Each author’s full name; institution(s) with which each author is affiliated, with city, state/province, zip code, and country; and the name, complete mailing address, telephone number, facsimile number (if available), and email address for all correspondence.

(3) You must put at least one email address under the authors’ address.

(4) Abstract: including Background, Materials and Methods, Results, and Discussions, 100-300 words preferred.

(5) Key Words.

(6) Introduction.

(7) Materials and Methods.

(8) Results.

(9) Discussions.

(10) Acknowledgments.

(11) Correspondence to.

(12) References.

Description of Manuscript Preparation and Format:

(1) Software: Microsoft Word file.

(2) Font: Normal, Times New Roman, 10 pt, single space.

(3) Indent: 8 spaces in the beginning of each new paragraph.

(4) Manuscript: Don’t use “Footnote” or “Header and Footer”.

(5) Spelling check: Do spelling check when you finish.

(6) Color: Email and website addresses are blue, and all other contents are black.

http://www.americanscience.org americansciencej@gmail.com

78

(7) Abstract: 100-300 words are preferred, and remember to add “[The Journal of  American Science. 2009;x(x):xx-xx]. (ISSN 1545-1003)” in the end of abstract.

(8) Page setup: Margins: top 72 pt, bottom 72 pt. left 72 pt, right 72 pt.

(9) Paper size: Letter, width 612 pt, height 792 pt.

(10) Layout: Header 36 pt, Foot 36 pt.

(11) Title: Use Title Case in the title and subtitles, e.g. “Debt and Agency Costs”.

(12) Figures and Tables: Use full word of figure and table, e.g. “Figure 1. Annul Income of Different Groups”, Table 1. Annual Increase of Investment”.

(13) References: Cite 10-20 references preferred, by “last name, year”, e.g. “(Smith, 2003)”. References should include all the authors’ last names and initials, title, journal, year, volume, issue, and pages etc.

(14) Reference Examples: Journal Article: Hacker J, Hentschel U, Dobrindt U. Prokaryotic chromosomes and disease. Science 2003;301(34):790-3.

(15) Book: Berkowitz BA, Katzung BG. Basic and clinical evaluation of new drugs. In: Katzung BG, ed. Basic and clinical pharmacology. Appleton & Lance Publisher. Norwalk, Connecticut, USA. 1995:60-9.

(16) Insert page number by bottom / center.

(17) Header for odd: Marsland Press, Journal of American Science 2009;x(x):xx-xx.

(18) Header for even: short title, Family name of the first author, et al.

(19) Footer: http://www.americanscience.org americansciencej@gmail.com.

(20) Submission Address: sciencepub@gmail.com, editor@sciencepub.net, Marsland Press, P.O. Box 21126, Lansing, Michigan 48909, The United States, 347-321-7172.