Nature and Science, 2012;10(4)	http://www.sciencepub.net/nature

Studies in Adsorption: Determination of Specific Surface Area of Aluminum, Stannous and Vanadium 
	Ferrocyanides by a Cationic Organic Dye Adsorption

Rawle Wayne Webster and Brij Bhushan Tewari

Department of Chemistry, University of Guyana, PO Box: 101110, Georgetown, Guyana. 
	brijtew@yahoo.com

Abstract: The present paper deal with the determination of specific surface area of aluminum, stannous and vanadium ferrocyanides by solution adsorption of methylene blue a cationic organic dyestuff at room temperature (30 ± 1ºC).  The adsorption of methylene blue solution was studied in pH range (2.0 - 10.0) and at concentration of 10-5 - 10-6 M.  The process was very fast initially and maximum adsorption was attained within 6 h of contact time. The experimental data are fitted to the Langmuir isotherm equation and value of corresponding constant was determined from the slope and intercept of the plot. Methylene Blue Dye (MBD) appears to be adsorbed flatwise from water with an effective molecular area of 130Å2. The Specific Surface Area (SSA) has been calculated. The SSA of particle size 125 µm was found to be 46.36 ± 0.05, 69.00 ± 0.11 and 81.42 ± 0.07 m2g-1 for aluminum, stannous and vanadium ferrocyanides , respectively.

[Rawle Wayne Webster and Brij Bhushan Tewari. Studies in Adsorption: Determination of Specific Surface 
Area of Aluminum, Stannous and Vanadium Ferrocyanides by a Cationic Organic Dye Adsorption. Nature 
and Science 2012;10(4):17-21]. (ISSN: 1545-0740). http://www.sciencepub.net/nature. 3

Keywords: Methylene blue dye; adsorption; metal ferrocyanides; Langmuir constants; specific surface area.

1.	Introduction

Dye adsorption data have been largely used 
for determination of specific surface area of solids 
(Brina, 1987) [1].  Dye adsorption, preferentially the 
uptake of methylene blue, has been often used as a 
substitute for BET measurement for determining the 
total surface of such compounds (Potgieter, 1991; 
Pekarek, 1972) [2, 3].  The measurement of SSA of 
finally divided solids becomes increasingly important 
in   laboratory   and   technical   processes. 	The 
determination of SSA of solids by solution adsorption 
is simple and has been shown to give reliable results 
with  a  wide  variety  of  solids.  Due  to  ease  of 
formation  of  cyanide  under  prebiotic  conditions 
(Beck, 1978) [4].  It is thought that insoluble double

- metal ferrocyanides were produced on the primitive 
earth due to interaction of cyanides with metal ions 
readily available in the environment.  These double -
metal   ferrocyanides   have   acted   as   adsorbents 
(Tewari, 1993; Tewari, 1998; Ali, 2006) [5-7], ion-
exchangers (Kourin, 1964;  Malik, 1976;  Bastian, 
1967) [8-10]  and  Photosensitizers (Tewari, 1996; 
Tewari, 1996) [11, 12].

A search of literature indicated that several 
report available on removal, kinetic, thermodynamic, 
equilibrium studies of adsorption of MBD on various 
adsorbents (Chen, 2011; Chaari, 2011; Ferrero, 2010; 
Wanchanthuek, 2011;  Hashemian, 2011;  Yadav, 
2011; Altaher, 2011; Wang, 2010; Annadurai, 2002; 
Froba, 2006) [13-22],  Some  report  available  on 
determination of SSA of various solids by MBD 
adsorption (Yukselen, 2006;  Avena, 2001;  Itodo,

17

2010; Santamarina, 2002; Tsai, 2011; Rubin, 2010; 
Inel, 	2000;   Shangareeva, 	2006;   Hang, 	1970; 
Kaewprasit, 1998; Kipling, 1960) [23-33], but no 
report   available   on   determination   of   SSA   of 
aluminum, stannous and vanadium ferrocyanides by 
MBD adsorption.  In view of this attempt has been 
made   to   determine   the   SSA   of   these   metal 
ferrocyanides.  In addition, present paper describes an 
MBD adsorption method for the determination of 
SSA   of   aluminum,   stannous   and   vanadium 
ferrocyanides.

2.	Experimental Section

2.1 Materials

Potassium ferrocyanide, aluminum chloride, stannous  chloride  and  sodium  vanadate  were obtained from BDH, Poole, UK.  Methylene blue dye was obtained from E. Merck, Darmstadt, Germany.  All chemicals used were of AnalaR grade.  Doubly distilled water was used for the preparation of solutions.

2.2   Synthesis of Metal Ferrocyanides 
	Aluminum  ferrocyanide  was  prepared  by

Kourim’s method (Kourim, 1964) [34] by adding 
slowly a potassium ferrocyanide (167 ml: 0.1 M) 
solution to a solution of aluminum (III) chloride 
(50 ml: 0.1 M) with constant stirring. Reaction 
mixture was heated onto a boiling waterbath for 
2-3 h and then cured for 24 h. The precipitate 
was filtered, washed with distilled water and 
dried in a oven at 60ºC.

Nature and Science, 2012;10(4)	http://www.sciencepub.net/nature

Stannous   ferrocyanide   was   prepared   by 
mixing   solution   of 	0.25 	M   potassium 
ferrocyanide and stannous chloride in ratio (2:1) 
(Tewari, 1995) [35].  The precipitate was cured 
at room temperature for 24h, filtered, washed 
and dried at 40ºC.

Vanadium    ferrocyanide    complex    was

stable  in  acids  (HCl,  HNO3,  H2SO4)  and  bases 
(NaOH 	, 	KOH,   NH4OH)   solutions   in   the concentration range 0.1 - 2.0 M.

Table 2. Infrared spectral data of aluminum, stannous and vanadium ferrocyanides

Adsorption frequencies (cm-1) 
Metal 	H2O

isolated (Baetsle, 1966; Huys, 1964) [36, 37] by 
adding (10  ml: 1.0  M)  HCl  to  a  mixture 
containing sodium vanadate (500 ml: 0.3 M) and 
potassium ferrocyanide (500 ml: 0.1 M) solution

ferrocyanidesa	molecules /

OH group

AlFc	3600

SnFc	3600 
VaFc 	3600

HOH	C ≡ N	Fe-	Metal

bending	Stretching	C	- Nb

1660	2000	600	490

1600	2000	600	500 
1600 	2040 	600 	490

with constant stirring.  Reaction mixture to be 
heated on a boiling water bath for 3 h to 4 h and 
then  allowed  to  cool  at  room  temperature 
overnight.  The precipitate formed was formed 
was filtered and dried at 50 ºC.  The dried 
products were ground and sieved to 125 µm 
mesh size.

2.3	Characterization of Metal Ferrocyanides

Aluminum,    stannous    and    vanadium

ferrocyanides are found to have light blue, dark 
blue  and  green  colour,  respectively.  These 
complexes are amorphous solid and show no X-
ray pattern.  All three metal ferrocyanides were 
characterized on the basis of elemental analysis 
and   spectral   studies.   Aluminum,   stannous, 
vanadium and iron were estimated by atomic 
adsorption IL-751 spectrophotometer - carbon, 
hydrogen and nitrogen analysis was performed 
on CEST-118, CHN analyzer.

Table 1. Elemental analysis of aluminum, stannous and vanadium ferrocyanides

b Metal - N band shows degree of polymerization

2.4	Adsorption Studies

The adsorption of MBD on metal ferrocyanides 
as a function of MBD concentration [10-5 - 10-6 M] 
was studied at room temperature (30 ± 1ºC) and pH

7.01 ± 0.01.  A series of 50 ml test tubes were employed.  Each tube was filled with 10 ml of MBD solution of varying concentration and adjusted to desired pH appropriate buffer.  Metal ferrocyanide (50 mg) was added to each tube and agitated for 24 h. Equilibrium  was  attained  in  about 6  h.    The equilibrium  time  and  concentration  ranges  were however decided after a good deal of preliminary investigations.  The concentration of MBD solution before   and   after   adsorption   was   measured spectrophotometrically at λmax 665 nm.

Figure 1. Effect of pH on adsorption of methylene blue dye on metal ferrocyanides.

Metal	Percentage Found

ferrocyan	Metal	Iron	Carbon	Hydrogen	Nitrogen

idesa

AlFc	9.90	11.10	13.20	4.90	16.60

SnFc	38.75	10.90	14.25	1.75	18.10

VaFc	24.10	13.90	18.10	2.00	19.73

Temperature = 30 ± 1ºC; amount of MFc = 50 mg;

AlFc = aluminum ferrocyanide; 
SnFc = Stannous ferrocyanide; 
VaFc = Vanadium ferrocyanide.

The values are given in Table 1.  All three metal 
ferrocyanides show a broad peak at around 3650 cm-
1, characteristic of water molecule and OH group. 
Also, a peak at around 1600 cm-1 due to  HOH 
bending  appeared  in  all  the  metal  ferrocyanides 
studied.  Two sharp bands at 2100 cm-1 and 600 cm-1 
are characteristics of cyanide and Fe-C stretching, 
respectively.  Another sharp band at around 500 cm-1 
probable show the presence of metal - nitrogen band 
due to polymerization.  The infrared spectral data are 
given in Table 2.  Metal ferrocyanides are found to be

particle size = 125 µm; λmax MBD = 665 nm.

3.	Results and Discussion

The   variation   of   adsorption   of   MBD   on aluminum,  stannous  and  vanadium  ferrocyanides with varying hydrogen ion concentration is given in Figure 1.  The percentage adsorption was calculated by the general formula

difference in concentration of MBD 
	before and after adsorption

% Adsorption =	x	100

concentration of MBD 
	before adsorption

18

Nature and Science, 2012;10(4)	http://www.sciencepub.net/nature

Aluminum and stannous ferrocyanide showed 
maximum adsorption  at  pH  2.0,  while  vanadium 
ferrocyanide has maximum adsorption at pH 3.0. 
The  percentage  uptake  of  MBD  on  aluminum, 
stannous and vanadium ferrocyanides is given in 
Table 3.

Table 3. Percentage adsorption of methylene blue on metal ferrocyanides

pH	Percentage adsorption

AlFc	SnFc	VaFc

2.0	98.08	49.25	93.25

3.0	58.68	35.80	96.46

4.0	77.75	27.15	92.60

5.0	95.83	24.35	91.85

6.0	66.46	22.30	85.27

7.0	42.32	48.65	89.10

8.0	55.72	40.50	87.43

9.0	52.57	12.86	74.55

10.0	47.25	9.00	77.10 
Room temperature = 30±1ºC; amount of MFc’s = 
50mg; λmax methylene blue dye = 665 nm; particle 
size = 125 µm.

A neutral pH was chosen to run the adsorption 
isotherms of the methylene blue dye in a wide range 
of  concentration  because  most  biological  redox 
reactions takes place in neutral medium.  Adsorption 
isotherm as Ceq (equilibrium adsorbate concentration 
versus q (amount mg of adsorbate adsorbed per gram 
of   adsorbent)   for   the  adsorption   of   MBD   on 
aluminum, stannous and vanadium ferrocyanides is 
shown in Figure 2.

Figure 2. Adsorption isotherm of methlyene blue dye on metal ferrocyanides.

Temperature = 30 ± 1ºC; pH = 7.0 ± 0.01; amount of 
MFc = 50 mg; particle size = 125 µm; λmax MBD = 
665 nm.

The isotherms are positive and concave to the 
concentration axis.  At low concentration adsorption 
is rapid, then slows down at higher concentration

until  adsorption  becomes  constant  and the  graph levels off.  This leveling off or ‘plateau’ indicates the saturation point (point at which maximum uptake of dye).  The order of maximum uptake of MBD on metal ferrocyanides at neutral pH is as follows:

Vanadium	stannous	aluminum 
ferrocyanide  >   ferrocyanide  >   ferrocyanide

Adsorption isotherm data have been analyzed in terms   of   the   Langmuir   isothermal   adsorption equation (Langmuir, 1918) [38].

Ceq                1                Ceq

Qeq               bQo             Qo

1              1             1            1

Qeq                Ceq              bQo            Qo

Where Ceq is the equilibrium concentration of 
MBD; b, a constant related to enthalpy (ΔH) of 
adsorption (b α e-∆HIRT); qeq, the amount (mg) of 
solute adsorbed per gram weight of adsorbent and Q0 
is the amount (mg) of  solute required per gram 
weight of metal ferrocyanides.  Langmuir plots for 
adsorption of MBD on metal ferrocyanides are shown 
in Figure 3.

Figure 3. Langmuir plots of methylene blue dye on metal ferrocyanides.

Temperature = 30 ± 1ºC; pH = 7.0 ± 0.01; amount of 
MFc = 50 mg; particle size = 125 µm; λmax MBD = 
665 nm.

All three Langmuir plots are liniar in behavior. The  values  of  Q0  and  b  were  determined  from intercept  and  slope  of  Langmuir  plot  and  are presented in Table 4.

The   approximate   specific   surface   area   of 
aluminum, stannous and vanadium ferrocyanides has

19

Nature and Science, 2012;10(4)	http://www.sciencepub.net/nature

been obtained with the help of following equation (Giles, 1970; Giles, 1964; Giles, 1962) [39-41]

Specific Surface Area(SSA)= 6.02 x 10-2 Mf Am (m2g-1)

Where Mf = m Mole of MBD adsorbed per 100 
gram  metal  ferrocyanides,  when  the  surface  is 
covered with monolayer, Am = area per molecule in 
Å2 on the surface. Under the condition of optimum 
flocculation, the area per adsorbed molecule of MBD 
is taken as 130Å2, which corresponds to the molecule 
lying flat on the adsorbent surface.  The calculated 
SSA values of metal ferrocyanides are given in Table 
4. 	It  is  observed  from  Table 4  that  vanadium 
ferrocyanide   and   aluminum   ferrocyanide   have 
maximum and minimum surface area, respectively.

Table  4.  Langmuir  constants  for  adsorption  of methylene blue dye on metal ferrocyanides

Langmuir 
Specific 	constants

methods reported in chemical literature for the determination of SSA of solids.

Corresponding Author: Dr. Brij B. Tewari

Professor

B.Sc., M. Sc., D. Phil., FRSC

Tel:	592-222-4926

Cell:	592-668- 6072

Fax:	592-222-3596 
E-mail:  brijtew@yahoo.com 
E-mail:  brijtewari2011@yahoo.com

References

[1]	Brina R, DeBattiste A. Determination of the Specific

Surface Area of Solids by Means of Adsorption Data.

J. Chem. Edu. 1987: 64(2): 175-176.

[2]	Potgieter, J. H. Adsorption of Methylene Blue on

Activated Carbon. J. Chem. Edu. 1991: 68(4): 349-
350.

Metal

ferrocyanides

AlFc 
SuFc 
VaFc

Particle 
	size

( µm)

125

125

125

surface	b x

area	105

(m2 g-1)	(liters

/ mol)

46.36 ± 	1.00 ±

0.05	0.02

69.00 ± 	0.72 ±

0.11	0.09

81.42 ± 	0.49 ± 
	0.07 	0.03

Q0 x 
	102

(mg/g)

0.83 ± 
	0.06

1.39 ± 
	0.01

2.50 ± 
	0.11

[3]	Pekarek   V,   Vesely   V.   Synthetic   Inorganic   Ion

Exchanges - II, Salts of Heteropolyacids, Insoluble

Ferrocyanides,	Synthetic    Aluminosilicate    and 
Miscellaneous   Exchanges.   Talanta 1972: 19(11): 
1245-1283.

[4]	Beck MT in: Sigel H (Ed.) Metal Ions in Biological

Systems, Marcel Dekker, New York 1978: No. 7: P. 1 
[5] Tewari    BB,    Kamaluddin    Interaction    of    o-
	Aminophenol and o-Nitrophenol with Copper, Zinc,

Room temperature = 30 ± 1ºC; pH = 7.0 ± 0.01; amount   of  metal  ferrocyanide = 50   mg;  λmax methylene blue = 665 nm.

It is also observed from Table 4 that vanadium 
ferrocyanide have highest Qo and lowest b value, 
while aluminum ferrocyanide have lowest Q0 and 
highest b values among all three metal ferrocyanides 
studied.

4.	Concluding Remarks

a)   All three metal ferrocyanides showed maximum 
	percentage uptake at very low pH level.

b)   Vanadium  ferrocyanide  is  considered  to  be

more porous in comparison to aluminum and stannous ferrocyanide.

c)   Present study conclude that adsorption of MBD 
	on metal ferrocyanides is quite satisfactory.

d)   Results of present study suggest the potential

use of MBD in the determination of SSA of metal ferrocyanides.

e)   The use of basic MBD for the determination of 
	SSA is more useful, because it is highly pure

and suitable for immediate use, as this dye is easily analyzed spectrophotometrically.

f)   Determination of SSA by MBD adsorption is 
	simple, rapid and reliable, therefore the present

method has significant advantages over other

20

Molybdenun and Chromium Ferrocyanides.  J. Colloid Interface Sci. 1993: 193: 167-171.

[6]	Tewari BB, Mohan D, Kamaluddin, Interaction of 2,

4-Dinitrophenol   and  2,	4,	6-Trinitrophenol   with

Copper,    Zinc,    Molybdenum    and    Chromium Ferrocyanides. Colloids and Surfaces A: Physicochem. Eng. Aspects 1998: 131: 89-93.

[7]	Ali SR, Kamaluddin, Interaction of Aromatic Amino

Acids with Metal Hexacyanoferrate(II) Complexes: A

Possible Role in Chemical Evolution. Bull. Chem. Soc. Jpn 2006: 79(10): 1541-1546.

[8]	Kourim V, Rais J, Stejskal J. Exchange Properties of

Complex Cyanides - II, Ion - Exchange of Alkali

metals on Zinc Ferrocyanide. J. Inorg. Nucl. Chem. 1964: 26: 1761-1764.

[9]	Malik WU, Srivastava SK, Bhandari VM, Kumar S.

Ion Exchange Properties of Chromium Ferrocyanides.

J. Inorg. Nucl. Chem. 1976: 38 :342-343.

[10] Bastian J, Lieser KH, Ion Exchange Properties of an 
	Titanium hexacyanoferrate(II) J. Inorg. Nucl. Chem.

1967:29: 827-832.

[11] Tewari B B, Kamaluddin, Photo-Sensitized Oxidation 
	of Diphenylamine using Nickel Ferrocyanide and its

Relevance  to  Chemical  Evolution.  Proceedings  of 
Ninth National Space Science Symposium (NSSS -
96), Osmania University , Hyderabad, India, 1996: P. 
93

[12] Tewari B B, Kamaluddin, Photosensitized Oxidation 
	of    Diphenylamine    in    Presence    of    Copper

Ferrocyanide. Proceedings of Eighty Third Session of 
the Indian Science Congress, Patiala, India 1996: p. 34

Nature and Science, 2012;10(4)	http://www.sciencepub.net/nature

[13] Chen YM, Tsao TM, Removal of Crystal Violet and 
	Methylene Blue from Aqueous Solution Using Soil

Nano	-Clays,   Proceedings   of   Conference   on Environmental  Science  and  Engineering,  IACSTT Press, Singapore 2011: 8: 252 - 254.

[14] Chaari I, Medhioub M, Jamoussi F. Use of Clay to 
	Remove Heavy Metals from Jebel Chakir Landfill

Leachate, J. Appl. Sci. Environ. Sanitation 2011: 6(2): 143-148

[15] Ferrero   F.   Adsorption   of   Methylene   Blue   on 
	Magnesium   Silicate:   Kinetics,   Equilibrium   and

Comparison with other Adsorbents. J. Environ Sci. 2010: 22(3): 467-473.

[16] Wanchanthuek R, Thapol A. The Kinetic Study of 
	Methylene Blue Adsorption Over MgO from PVA

Template Preparation. J. Environ. Sci. Technol. 2011: 4(5): 552-559.

[17] Hashemian   S.   Kinetic   and   Thermodynamic   of 
	Adsorption of Methylene Blue by Cu2Fe2O4 / Rice

Bran Composite. Int. J. Phys. Sci. 2011: 6(27): 6257-
6267.

[18] Yadava S, Tyagi DR, Yadava OP, Equilibrium and 
	Kinetic Studies on Adsorption of Aniline Blue from

Aqueous Solution onto Rice Husk Carbon. Int. J. Chem. Res. 2011: 2(3): 59-64.

[19] Altaher H, Elqada E. Investigation of the Treatment of 
	Colored  Water  Using  Efficient  Locally  Available

Adsorbents, Int. J. Energy Environ. 2011: 2(6): 1113-
1124.

[20] Wang XS. Removal of Basic Dye (Basic Magenta) 
	Using Low Cost Biosorbents from Aqueous Solutions:

Kinetic  and  Equilibrium  Studies.  Int.  J.  Environ. Technol. Manage. 2010: 12(2-4): 151-162.

[21] Annadurai G, Juang RS, Lee DJ. Removal of Dye by 
	Banana and Orange Peels Use of Cellulose based

Wastes for Adsorption of Dye from Aqueous Solution.

J. Hazard. Mater. 2002: B92: 263-274.

[22] Froba  M.  Silica  -  Based  Mesoporous  Organic  -

Inorganic   Hybrid   Materials:   Review  Mesoporous

Materials. Angew. Chem. Int. Ed. 2006: 45: 3216-
3251.

[23] Yukselen Y, Kaya A. Comparison of Methods for 
	Determining  Specific  Surface  Area  for  Solids.  J.

Geotech. Geoenviron. Eng. 2006: 132(7): 931-937. 
[24] Avena  MJ,  Valenti  LE,  Pfaffen  V,  DePauli  CP.

Methylene Blue Dimerization does not Interfere in Surface Area Measurement of Kaolinite and Soils. Clays Clay Miner. 2001: 49(2): 168-173.

[25] Itodo  AU,  Itodo  HU,  Gafar  MK.  Estimation  of 
	Specific  Surface  Area  using  Langmuir   Isotherm

Method. J. Appl. Sci. Environ. Manage. 2010:14(4): 141-145.

[26] Santamarina JC, Klein KA, Wang YH, Prenche E. 
	Specific Surface: Determination and Relevance Can.

Geotech. J. 2002:39: 233-241.

[27] Tsai    WT,    Chen    HR,    Kuo    KC.    Surface 
	Characterization of Dead Microalgal - Based Biomass

Using  Methylene  Blue  Adsorption.  Surf. Interface Anal. 2011: 43(6): 959-963.

[28] Rubin E, Rodriquez P, Herrero R, Sastre de Vincente 
	ME. Adsorption of Methylene Blue on Chemically 
	Modified Algal Biomass: Equilibrium, Dynamic and

Surface Data. J. Chem. Eng. Data 2010: 55(12): 5707-
5714.

[29] Inel O, Tumsek F. The Measurements of Surface Area 
	of Some Silicates by Solution Adsorption. Turk J.

Chem. 2000: 24: 9-19.

[30] Shangareeva  OV,  Fedoseeva  VI,  Fedoseeva  NF. 
	Determination of Specific Surface Area of FORUM

Fluoroplastic Powder by the Dye Adsorption from Solutions.  Colloid J. 2006: 68(5): 651-653.

[31] Hang PT, Brindley GW, Methylene Blue Adsorption 
	by Clay Minerals.  Determination of Surface Areas

and   Cation   Exchange   Capacities  (Clay   Organic 
	Studies XVIII). Clays Clay Miner. 1970:18: 203-2012. 
[32] Kaewprasit  C,  Hequet  E,  Abidin  N,  Gourlot  JP.

Application of Methylene Blue Adsorption of Cotton Fibre Specific Surface Area Measurement: Part - I Methodology. J. Cotton Sci. 1998: 2: 164-173.

[33] Kipling J. J, Wilson R. B, Adsorption of Methylene

Blue in the Determination of Surface Areas. J. Appl. Chem. 1960: 10(3): 109-113.

[34] Kourin V, Rais J and Million B. Exchange Properties 
	of Complex Cyanides - I. J. Inorg. Nucl. Chem.

1964:26: 1111 - 1115.

[35] Tewari BB, Mohan D, Kamaluddin, Srivastava SK. 
	Determination of Specific Surface Area of Copper,

Zinc, Stannous and Molybdenum Ferrocyanides by 
Dye Adsorption. Indian J. Chem. Technol. 1995: 2: 
113-114.

[36] Baetsle  LH,  Huys  D,  Deyck  DV.  Ferrocyanide 
	Molybdate, A New Inorganic Ion Exchanger(II). Ion

Exchange  and  Radiochemical Properties. J.  Inorg. Nucl. Chem. 1966:28: 2385-2394.

[37] Huys D, Baetsle LH. A New Series of Synthetic Acid 
	Stable Mineral Ion Exchanger - I. Ferrocyanide -

Molybdate (FeMo). J. Inorg. Nucl. Chem. 1964: 26 : 1329-1331.

[38] Langmuir I. The adsorption of Plane Surface of Glass, 
	Mica and Platinum. J. Am. Chem. Soc. 1918: 40:

1361-1403.

[39] Giles  CH,  D’Silva  AP,  Trivedi  AS,  Use  of  p-
	Nitrophenol  for  Specific  Surface  Measurement  of

Granular Solids and Fibres. J. Appl. Chem. 1970: 20: 
37-41.

[40] Giles CH, Tolia AH. Studies in Adsorption. XIX. 
	Measurement of External Specific Surface Area of

Fibres by Solution Adsorption. J. Appl. Chem. 1964: 14: 186-195.

[41] Giles CH, Nakhwa SN. Studies in Adsorption. XVI. 
	The Measurement of Specific Surface Areas of Finally

Divided Solids Solution Adsorption. J. Appl. Chem. 1962: 12: 266-273.

2/12/2012

21