Beneficiation Processing of Agbaja Iron Ore By Chemical Leaching Technique

S.M.O. Obiorah1, M.C.Menkiti2*, E.E.Nnuka1

1Department of Material and Metallurgical Engineering, Nnamdi Azikiwe University, Awka, Anambra State,  Nigeria

2Department Of Chemical Engineering,  Nnamdi Azikiwe University, Awka, Anambra State,  Nigeria

*Corresponding author: cmenkiti@yahoo.com

ABSTRACT: The effects of dwell time, dilution ratio, leachant concentration and variables interaction on the dephosphirization of Agbaja iron ore have been investigated by chemical leaching[H2SO4] technique and 23- factorial surface response methodology. Results indicate 96%, 95% and 96% of phosphorus removal at 36 min leaching time,0.3M leachant concentration and 1:2 dilution ratio, respectively. Iron loss during the leaching was less than 0.15%.It can be concluded that acid leaching of Agbaja iron ore is feasible at the conditions of the experiment.

[S.M.O. Obiorah, M.C.Menkiti, E.E.Nnuka. Beneficiation Processing of Agbaja Iron Ore By Chemical Leaching Technique. New York Science Journal 2011;4(5):22-27]. (ISSN: 1554-0200). http://www.sciencepub.net/newyork.

KEYWORDS: Agbaja, Leaching, Iron, Ore, Beneficiation,Iron ore

INTRODUCTION

Nigeria is one of the richest countries of the world in terms of mineral deposits. Among these deposits is iron ore, located at Agbaja, Kogi State, Nigeria. Agbaja iron ore deposit, the largest in Nigeria is about 1.3billion tones. Agbaja iron ore is of low silicon modulus (SiO2/Al2O3), fine texture and and contains about 1.4-2.0% phosphorus. The prevalence of this amount of phosphorus is a major set back to its utilization in the blast furnace or direct reduction process (Alafara et al,2005).

The removal of phosphorus from iron and steel presents problems because of similarity of the standard free energies of formation of iron oxide and phosphorus pentoxide (Alafara et al,2005). Consequently, in the reducing conditions of the blast furnace to recover some 99.5% of the iron charged, near complete reduction of phosphorus pentoxide from the acid blast furnace occurs. As the phosphorus in the ore impregnates the pig iron, there occurs two distinct processes of tackling the problem: pyrometallurgical route and hydrometallurgical route. The first route employs basic slag during the conversion to steel. This  technique covers the activity coefficient of phosphorus pentoxide in the slag(Alafara et al,2005; Alafara et al,2003; Li and Wen,2004; Whiteley,1923).The second route delves into ways of reducing phosphorus in the iron at relatively low temperatures.

Leaching of lean ores or complex ore in different acids has proved  successful for several years. However, the leaching of phosphorus contaminated iron ore has made a very limited progress. This underscores the ongoing intense research in the area for several decades. Depending upon the degree of association of phosphorus with the minerals in the iron body, iron ore can be beneficiated in either of the three ways: smelting process, physical separation and chemical leaching (Kokal,1990).

As is well known, smelting process is effective for  dispersion but with very high cost, and it is still under fundamental research. For physical separation, communition followed by wet magnetic separation or froth flotation is generally employed when the phosphatic gangue mineral appears as discrete inclusion in the iron body matrix(primary mineralization)(Kokal,1990; Kokal et al,2003;Fonesca et al,1994). Low phosphorus extraction, high grinding cost and iron loss are the major disadvantages of the method. However, when phosphorus is disseminated in the iron structure, possibly forming cryptocrystalline phosphates or solids solutions with the iron oxide phases (secondary mineralization), the beneficiation can only proceed by chemical routes (Kokal,1990; Kokal et al,2003; Forsberg and Asolfesson, 1981).

Forsberg and Asolfesson(1981); Cuj and Fang(1998); Hang et al,(1994); He and Zhou,(2000); Balajiva et al,(1946); investigated dephosphorization with acid leaching. In their studies,the acid concentrations were very high and low phosphorus extraction were obtained. In this study, the feasibility of dephosphorizatin of Agbaja iron ore by  acid leaching at various dilution ratio, dwell time and particle size were investigated. Also, the Design of Experiment for the evaluation of  interactive factorial effects on the phosphorus removal was also investigated.

MATERIALS AND METHOD

Sample Collection

Iron Ore samples of 0.40mm particle size of Agbaja iron ore were collected from National Metallurgical Development Centre( N M D C), Jos, Plateau State, Nigeria. The samples were stored in a dry environment for analysis after being sieved to produce particle size fraction of  0.2-0.4mm.

Determination Of Iron And Phosphorus Phase Content Of Untreated Ore

The phases in which iron and phosphorus phases were present within the iron ore were determined by x-ray diffraction(XRD) analysis and atomic  absorption spectrophotometry.

Chemical Preparation Of Leaching Solution

All leaching chemicals used were of laboratory grade, procured from Bridge Head Chemical Market, Onitsha, Nigeria. 1M leaching solutions of sulphuric acid were prepared by diluting the concentrated form of the acid in distilled water. The dilution ratios employed were 1:0,1:1,1:2,1:3,1:4,1:5,1:6.

Chemical Leaching Procedure

Cotton wool was rammed into the bottom part of chromatographic column followed by the introduction of fine granules of crushed ceramics. Thereafter, 0.4mm of 20g of Agbaja iron ore was introduced into the tube and the tube clamped. 100ml of 1M H2SO4   was introduced into the clamped column containing the 20g iron ore. A conical flask is placed beneath the column to receive the leach liquor. The leaching time and leachant  dilution were varied at 31oC ,0.4mm particle size. At the end of each leaching treatment, the residue was removed from the column and washed for 3 times with distilled water. The treated ore samples were dried in oven at 150oC for 24 hours. The respective leached liquor were stored in flask for phosphorus content analysis.

Design Of  Experiment For The Leaching

Statistically designed experiment was conducted for  the leaching treatment based on 23  full factorial design. The design matrix for the three variables, two levels and eight experimental runs and responses are shown below:

| Table 2.1: Design matrix of DOE and responses. |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| S/NO | X0 | X1 | X2 | X3 | Yave(mg/g) |
| 1 | +1 | -1 | -1 | -1 | 7.75 |
| 2 | +1 | +1 | -1 | -1 | 15.0 |
| 3 | +1 | -1 | +1 | -1 | 15.50 |
| 4 | +1 | +1 | +1 | -1 | 15.00 |
| 5 | +1 | -1 | -1 | +1 | 7.75 |
| 6 | +1 | +1 | -1 | +1 | 6.50 |
| 7 | +1 | -1 | +1 | +1 | 5.55 |
| 8 | +1 | +1 | +1 | +1 | 4.35 |

Also, shown below is the experimental range and levels of independent process variables.

Table 2.2: Experimental range and levels of Independent process variables.

| Independent Variable | Lower limit (-1) | Base level (0) | Upper limit (+1) |
| --- | --- | --- | --- |
| Dilution ratio | 0.20 | 0.60 | 1.00 |
| Particle size | 0.20 | 0.40 | 0.60 |
| Dwell time | 20.00 | 30.00 | 40.00 |

RESULTS AND DISCUSSION

X-Ray diffraction (XRD) analysis of  the untreated ore revealed the major mineral phases present as hematite (hematite), quartz  (Si2O3), alumina(Al2O3) and phosphorus pentoxide( PO5)  while the X-ray  fluorescence spectroscopy (XRF) and atomic absorption spectroscopy (AAS) revealed the chemical composition as shown in table 3.1. Since phosphorus contained within the iron ore is non-sulphidic phase, acid leaching presents the best option for its removal.

Effect  Of  Leaching time

The summarized effects of acid leaching time on dephosphorization of  the ore samples  are shown in table 3.2. From the table, it could be seen that the phosphorus removal from the ore  reached maximum values of about 96% at 36 minutes during the  leach process. The results indicate that as the leaching time decreases,there is corresponding decrease in the amount of phosphorus removed.

Effect of  Leachant Concentration

The effects of leachant concentration is presented in table 3.3 for samples A-B. There was increment  in  percentage of   leached liquor as the leachant concentration increased from 0.13-0.3M. Above 0.3M, the % phosphorus decreased from 92% to 47%. The  maximum phosphorus removal of  95%  was achieved at 0.3M leachant concentration. The initial low phosphorus removal using the concentrated acid could be due to cations present(Forsberg and Asolfesson,1981).

Effect Of Acid Dilution Ratio

The effect of acid dilution ratio is shown in 3.4. From the table, it can be shown that phosphorus extraction increases as the dilution ratio increases and reaches a maximum at 1:2 dilution of the H2SO4  corresponding to maximum of 96% phosphorus removal. As the dilution ratio increased further, there was a progressive decrease in phosphorus extraction.

Iron  Loss During Leaching

Iron loss recorded after the  leaching process is shown in table 3.5.It can be seen that iron content in the leachate(leached liquour) decreases as the dilution ratio increases. Quantitatively, it can be shown that iron loss is less than 0.1%, an amount that can be practically considered negligible.

DOE  Interaction  Effects  And  Responses

A 2 3 full factorial experimental design with two replications generated 16 experiments employed in this study. The design matrix is shown in table 2.1. The parameters: dilution ratio(X1), particle size(X2) and dwell time(X3) were chosen as independent variables at two levels while phosphorus removal is the output response. The   analysis is  focused  on how the phosphorus removal (dependent output variable) is influenced by the independent variables, i.e.  X1, X2  and X3.  The dilution ratio range studied was between 0.2 and 1, particle size varied between 0.2  and 0.6mm and dwell time in the range of 20 to 40min as shown in table 2.2. In order to study the combined effect of these factors, experiments were performed at different combinations of the physical parameters using statistically designed experiments. Upon the determination of polynomial coefficients, statistical analysis (CSI,G-Test,F-Test,T-Test) were performed to develop model that is adequate, significant and homogeneous(variance wise)(Menkiti,2010). The main effects of the parameters and response behavior of the system are explained by equation shown below:

Yu=9.675+0.493X1+0.425X2-3.637X3-.0.9625X1X2-1.150X1X3-1.512X2X3

The corresponding interactive surface response plots are presented in figures 1-3. Figure 1 shows the interaction effect of  dwell time and particle size on phosphorus removal. In respect of figure 2, the interaction effect of  dilution ratio and particle size is presented  while figure 3 shows the interaction effect of dilution ratio  and dwell time. It is important to note that the value of output responses are tied to the intensity of the colour of surface plots. The plots provide avenue to observe the surface area of the curve within which the process can perform at optimal level based on the effects of the interaction of the variables under consideration. The significance of these interaction effect between the variables would have been lost if the experiments was conducted by traditional method.

| Table 3.1: Major Elemental Composition of Agbaja Iron Ore Deposit |  |
| --- | --- |
| Major Elements | Mass (%) |
| Fe | 47.40 |
| SiO2 | 10.25 |
| Al2O3 | 11.35 |
| CaO | 0.88 |
| MgO | 0.22 |
| TiO2 | 0.31 |
| MnO | 0.15 |
| P2O5 | 1.60 |
| S | 0.07 |

| Table 3.2 : Effect of leaching time |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| S/NO | Sample |  | Leaching time (min) | Residue Wt(g) | % P in leached Liquour |
| 1 | A |  | 60.00 | 17.30 | 48.00 |
| 2 | B |  | 38.00 | 19.50 | 93.00 |
| 3 | C |  | 36.00 | 19.80 | 96.00 |
| 4 | D |  | 24.00 | 20.00 | 93.00 |
| 5 | E |  | 23.00 | 20.00 | 48.00 |
| 6 | F |  | 22.00 | 20.00 | 41.00 |
| 7 | G |  | 21.00 | 20.00 | 35.00 |
| 8 | H |  | 20.00 | 20.00 | 29.00 |

| Table 3.3 : Effect of leachant concentration |  |  |  |  |
| --- | --- | --- | --- | --- |
| S/NO | Sample | Leachant Conc (M) | Residue Wt(g) | % P in leached Liquour |
| 1 | A | 1.00 | 16.47 | 47.00 |
| 2 | B | 0.50 | 18.58 | 92.00 |
| 3 | C | 0.30 | 18.88 | 95.00 |
| 4 | D | 0.25 | 19.05 | 92.00 |
| 5 | E | 0.20 | 19.02 | 47.00 |
| 6 | F | 0.17 | 19.02 | 43.00 |
| 7 | G | 0.14 | 19.02 | 40.00 |
| 8 | H | 0.13 | 19.02 | 31.00 |

| Table 3.4 :Effect of dilution ratio on dephosphorization |  |  |
| --- | --- | --- |
| Specimen sample | Dilution ratio | % Conc of Phosphorous in the tailing |
| A | 1:0 | 48.00 |
| B | 1:1 | 93.00 |
| C | 1:2 | 96.00 |
| D | 1:3 | 93.00 |
| E | 1:4 | 48.00 |
| F | 1:5 | 41.00 |
| G | 1:6 | 35.00 |
| H | 1:7 | 29.00 |

| Table 3.5 : Iron loss from the leached liquor |  |
| --- | --- |
| Sample | ppm |
| A | 2.14 |
| B | 2.12 |
| C | 1.23 |
| D | 1.04 |
| E | 1.04 |
| F | 0.60 |
| G | 0.50 |
| H | 0.36 |

Figure 1: Surface / contour plot showing interaction effects of dwell time  and particle size on phosphorous removal  from ore.

Figure 2: Surface / contour plot showing interaction effects of dilution ratio  and particle size on phosphorous removal  from ore.

Figure 3: Surface / contour plot showing interaction effects of dwell time and dilution ratio on phosphorous removal  from ore.

REFERENCES

- Alafara A. B. and Adekola F. A.O. Bioline. Journal of Applied Sciences and Environmental Management, 2005:9(3):15-20.

- Alafara A.B., Adekola F.A., Mesubi M.A. and Bale R.B. Nigerian iron ore deposit. Journal of chemical society of Nigeria, 2003: 28(1): 40-44.

- Balajiva K., Quarell A.G. and Vajragiuta P. A. Laboratory investigation of the phosphorus reaction in the basic steelmaking process. J. Iron St. Inst., 1946: 153:115-145.

- Cuj J.and Fang Q.The present status and trends of dephosporizing of high phosphorus iron ore. Multipurpose utilization of mineral resources, Chicago, 1998:(6):20-24.

- Fonesca D., Souza C.and Araujo A. Hydrometallurgical routes for the reduction of phosphorus in iron ores. In  Wilkomirsky I., Sanchez M., Hecker,C. and Sutulov A. Eds.Chemical metallurgical, IV meeting of the Hemisphere on mineral Technology. Universidad de concepcion. Conception-Chile,  1994:Vol.III.:83-92

- Forsberg R. and Asolfesson G. Dephosphorisation of high-phosphorus iron resources by means of acid bleaching. Erzmetal 1981, 34:316-322.

- Hang J., Yang V. and Xie H. A study on the dephosphoristion of iron ore by phosphorus dissolving agent accompanied with thiobacillus. Journal of Nanjing forestry University, 1994: 18(2):25-29.

- He L.and Zhou J. Characteristics of Meishan iron ore with high phosphorus-bearing and feasibility of biodephoruzation. Gold Journal, 2000: 2(1):26-29.

- Kokal H.R. The origin of phosphorus in iron making raw materials and methods of removal.  AIME Proceeding, 51st Annual Mining symposium Duluth – Minnesota, January 17-18, 1990:225-258.

- Kokal R., Singh M.T. and Naygyonov V.A. Removal of phosphorus from the Lisakogsky Iron Ore by roast-leach process. In Young C.A. et al: Hydrometurlogy, Proceedings of fifth international symposium, 2003.

- Li X. and  Wen S. An overview of the presnt statues of dephosphirasation of iron. Metallic ore dressing abroad, 2004:41:4-7

- Menkiti M.C. Sequential treatments of coal washery and brewery effluents by biocoag-flocculation and activated carbon adsorption. Ph.D Theses, Chemical Engineering Department, Nnamdi Azikiwe University,Awka, Nigeria,2010.

- Rath P.C., Paramguru R.K. and Jena P.K.  Leaching of Iron Ore. Hydrometallurgy,1992: 7:5-9.

- Whiteley J. H. The Dephosphorization of iron in the basic furnace. Proc. Cleaveland Instn. Engr., 1923:59: 36-55.

- Zea Y.K. The phosphorus reaction in basic open heart practice.Iron and steel institute,1945:459-504.

4/13/2011